## Slide 1: PCB FABRICATION : FOR HIGH POWER ELECTRONICS

## Slide 2: EUCLIDS LABS,DEHRADUN
It is an R&D lab in Dehradun and currently they are working on developing efficient and inexpensive substitutes for Metal Clad Printed Circuit Boards (MCPCB) used in high power LED lights.
Start-up by Tarun Jha (CEO of Euclids Labs)

## Slide 3: PRINTED CIRCUIT BOARD(PCB)
A PCB is a thin board in which conductive pathways are fabricated onto board, connecting different components on the board such as transistors, resistors, and integrated circuits.
TOP VIEW
CROSS-SECTIONAL VIEW

## Slide 4: PCB MADE OF...
PCBS are made of
FR4
Flame Retardant
LIMITATIONS :
POOR FLEXIBILTY
POOR THERMAL CONDUCTIVITY(O.25-0.4 W/m.k)
Low Glass Transition Temperature ( 120-140 deg C)
Low luminous efficiency
Fibre glass reinforced epoxy

## Slide 5: Metal Clad Printed Circuit Board (MCPCB)
FR4
Aluminium or Copper substrate

## Slide 6: PCB v/s MCPCB (heat dissipation )

## Slide 7: INSULATED METAL SUBSTRATE (IMS)
Circuits are mounted directly on Al substrate.
More efficient and cheaper than PCBs and MCPCBs.
CROSS SECTIONAL VIEW

## Slide 8: MCPCB v/s IMS (heat dissipation)

## Slide 9: SCREEN PRINTING
Screen printing is a printing technique where a mesh is used to transfer ink onto a substrate, except in areas made impermeable to the ink by a blocking stencil.

## Slide 10: Mesh Classification
Mesh number: Number of opening per inch(linearly)of a mesh
LOW HIGH
Material type: Nylon , Polyester , Stainless Steel

## Slide 11: IMS Manufacturing Process
Substrate cleaning
Dielectric layer
a)Printing(100 mesh , snap off
+
Levelling (Room Temp 10 minutes )
b)Drying (150-200 degC 5-8 minutes)
+
Firing(at 570 degC 7minutes)
Conductor layer

## Slide 12: Project using KICAD
Schematic diagram of CLAP CIRCUIT

## Slide 13: Steps for Fabrication
Schematic diagram using KICAD.
Cleaning of copper board to remove oxidized layer.
Pattern transfer.
Etching using FeCl3.
Cleaning of ink.
Drilling of holes.
Soldering components.

## Slide 14: APPLICATIONS OF PCB

## Slide 15: REFERENCES
www.euclidlabs.in
Course-PCB fabrication
- Videos and study material by
Tarun Jha (CEO)